## Slide 1: Computer modelling of double doped SrAl2O4 for phosphor applications
Robert A Jackson*, Lauren A Kavanagh and Rebecca A Snelgrove
School of Physical & Geographical Sciences
Keele University
Keele, Staffs ST5 5BG, UK
*r.a.jackson@keele.ac.uk
@robajackson

## Slide 2: Motivation: paper based on presentation at EURODIM2014 by Philippe Smet

## Slide 3: Plan of talk
Background to the research
Aim of the research
3. Outline of methodology
4. Results
  Defect and solution energy calculations
  Single doping
  Double doping
  Mean field calculations
5. Future work & conclusions
6. Acknowledgements & reminiscences

## Slide 4: Background
SrAl2O4, when doped with Eu2+ and Dy3+ ions, behaves as a phosphor (the Dy3+ is found to enhance luminescence intensity).
It has many applications, e.g. in emergency signs.
SrAl2O4: Eu3+, Dy3+ synthesised by laser melting
After UV light exposure*
* ‘Laser Synthesis and Luminescence Properties of SrAl2O4: Eu2+, Dy3+ Phosphors’, Aroz et al, http://digital.csic.es/bitstream/10261/73706/4/Laser Synthesis.pdf

## Slide 5: Aim of the research
To predict the optimal doping locations for Eu2+ and Dy3+ ions.
  If, as suggested experimentally, Dy3+ substitutes at the Sr2+ site, how is the charge compensated?
  Most of the experimental papers do not discuss this!
Is double doping energetically favourable?
What is the effect of dopant concentration?

## Slide 6: Methodology
As in our previous work, use is made of interatomic potentials, energy minimisation and the Mott-Littleton method, using the GULP code*.
The structure of SrAl2O4 was modelled using potentials from http://www.ucl.ac.uk/klmc/Potentials/Library/catlow.lib
 | Exp.** | Calc. | %***
a | 8.44365 | 8.49801 | 0.64
b | 8.82245 | 9.03433 | 2.40
c | 5.15964 | 5.25031 | 1.76
= | 90.0 | 90.0 | 0.0
β | 93.411 | 92.425 | -0.99
**Avdeev et al, Journal of Solid State Chemistry (2007) 180, 3535-3544
*http://nanochemistry.curtin.edu.au/gulp
***Differences of a few % are a compromise due to using transferred potentials.

## Slide 7: Defect and solution energy calculations
Defect formation energies (including substitution energies) are calculated using the Mott-Littleton method (see opposite):
Solution energies give the energy involved in the total solution process, e.g. for Eu2+ at Sr site:
 Mark Read

## Slide 8: Intrinsic defect formation energies and lattice energies
Calculations of Schottky and pseudo-Schottky energies have been performed:
*M Rezende MSc thesis,
(2008)
 | Energy/eV
Sr vacancy | 19.53
Al vacancy | 59.26
O vacancy | 25.16
E (latt) SrAl2O4 | -194.4
E (latt) SrO | -33.97
Schottky (per ion) | 6.325
SrO pseudo-Schottky (per ion) | 5.330
(O Frenkel (per ion) | 5.180)*

## Slide 9: Single doping calculations – (i)
The experimental literature assumes doping of both Eu2+ and Dy3+ at the Sr2+ site (but doesn’t justify this in detail).
  Not a problem for Eu2+ where no charge compensation is required:
  The average solution energy is 0.06 eV, confirming that doping with Eu2+ is favourable.
For Dy3+, what about substitution at the Al3+ site?
  Assuming
  Solution energy is 1.72 eV (per Dy3+), which suggests the doping process at this site is favourable.

## Slide 10: Single doping calculations – (ii)
For Dy3+ doping at Sr2+, charge compensation is required. We assume this occurs via Sr2+ vacancy compensation:
  The calculated solution energy is 3.08 eV per Dy.
This suggests that single doping with Dy3+ at the Sr2+ site is less energetically favourable than if the ion substitutes at the Al3+ site, assuming charge compensation via Sr2+ vacancies.

## Slide 11: Double doping calculations
For doping with Eu2+ and Dy3+, assuming the following scheme (both ions at Sr sites, Sr vacancies):
The solution energy per dopant ion is 2.08 eV
  Double doping at the Sr2+ site is calculated to be more favourable than two stages of single doping.
  However, it is still predicted that Dy3+ ions will substitute at the Al3+ site, unless an alternative charge compensation scheme occurs.

## Slide 12: Comparison with an experimental study on M3+- doped SrAl2O4
This paper looked at the effect of M3+ doping on SrAl2O4 lattice parameters.
Occupation of the Sr2+ site by M3+ was assumed (again!) with no discussion of charge compensation.
‘Study on Optical Properties of Rare-Earth Ions in Nanocrystalline Monoclinic SrAl2O4: Ce3+, Pr3+, Tb3+’, Fu et al, J. Phys. Chem. B 2005, 109, 14396-14400

## Slide 13: Mean field calculations
These are perfect lattice calculations in which the occupancy of a dopant ion at a lattice site is steadily increased.
They enable the average effect of doping on lattice parameters etc. to be calculated.
If the dopant cation is not the same charge as the ion it is substituting, vacancies or interstitials are introduced by increasing or decreasing the anion charge to ensure a neutral unit cell.

## Slide 14: Mean field calculations on M3+- doped SrAl2O4
Doped material | a/Å
SrAl2O4: Ce3+ | 8.431
SrAl2O4: Pr3+ SrAl2O4: Tb3+ | 8.432 8.441
From the table:
Pure ‘a’ = 8.447 Å
If the M3+ ions are substituted at the Al3+ site, the calculations suggest expansion of the lattice.
So mean field calculations were carried out to assess average effect of doping, assuming substitution at the Sr2+ site.

## Slide 15: Results of mean field calculations
The calculations show that the ‘a’ lattice parameter contracts on doping with M3+ ions.
In these calculations, the charge was compensated by increasing the O charge, suggesting a preferred charge compensation scheme might be based on O interstitials.
The graph shows ‘a’ lattice parameter for the system:
Sr1-xMxAl2O4+x/2 as a function of x.
(Charge compensation by increased O charge.)

## Slide 16: Future work and conclusions
The results obtained so far demonstrate that relatively simple solution energy calculations have a useful role in helping interpret and further explain experimental data.
However, charge compensation is important and needs to be considered more in experimental papers!
Future work will look at finite dopant concentrations, using methodology still being developed, as well as by supercell calculations.

## Slide 17: Acknowledgements
I would like to thank:
My co-authors Lauren and Becky, both undergraduate students, who (without knowing it) are helping to keep my research alive (in austerity and pre-Brexit UK)!
Mário Valerio for many useful discussions over many years (32 years and counting!)
Christophe Dujardin and his team for organising this splendid conference.

## Slide 18: Reminiscences
The last ‘DIM’ conference in Lyon was in 1994. At that conference I was ‘assigned’ to organise the EURODIM 98 conference in Keele …